Hands on session:
PHONONS with Quantum ESPRESSO
Sharmila Shirodkar
Jawaharlal Nehru Centre for Advanced Scientific Research
Bangalore

---
Exercises
1. To calculate phonon frequencies at the Brillouin Zone centre (Γ-point) for silicon.
2. To calculate the phonon dispersion along high symmetry directions in the BZ for silicon.
3. To calculate the phonon frequencies in a polar material (AlAs), accounting for the presence of macroscopic electric fields and LO-TO splitting.
4. To calculate phonon dispersion of a metal (Al).

---
Exercise 1: phonon frequencies at Γ-point for silicon
- Executables: pw.x and ph.x
- Post processing: dynmat.x
  To run the script: nohup sh run.sh &
Look in run.sh for
the sequence
Step1: run a scf calculation on the equilibrium structure
 &electrons
    mixing_mode = 'plain'
    mixing_beta = 0.5
    conv_thr = 1.0d-10
 /
Smaller for scf calculations

---
Exercise 1: phonon frequencies at Γ-point for silicon
Step2: run a phonon calculation with ph.x
/usr/local/apps/espresso-5.1/bin/ph.x < si_ph_G.in > si_ph_G.out
 &inputph
   outdir='./tmp/',
   prefix='si',
   fildyn='si.dynmat_G',
   tr2_ph=1.0d-14,
   amass(1)=28.086
 /
0.0 0.0 0.0
Path to temporary folder of scf
Prefix used in scf calculation
Name of file for saving dynamical matrix
Minimum threshold for convergence or smaller
Atomic mass of each atomic type:
If not specified it is read from the data file
q point at which frequencies are calculated (in 2pi/a format)

---
Exercise 1: phonon frequencies at Γ-point for silicon
In the output of ph.x: si_ph_G.out
    omega( 1) = 0.437450 [THz] = 14.591747 [cm-1]
    omega( 2) = 0.437450 [THz] = 14.591747 [cm-1]
    omega( 3) = 0.437450 [THz] = 14.591747 [cm-1]
    omega( 4) = 14.994107 [THz] = 500.149581 [cm-1]
    omega( 5) = 14.994107 [THz] = 500.149581 [cm-1]
    omega( 6) = 14.994107 [THz] = 500.149581 [cm-1]
Acoustic
modes
Optical
modes
The frequencies of acoustic modes at BZ centre are supposed
to be zero due to translational invariance

---
Exercise 1: phonon frequencies at Γ-point for silicon
In the si.dynmat_G file
     q = ( 0.000000000 0.000000000 0.000000000 )
 **************************************************************************
     omega( 1) = 0.437450 [THz] = 14.591747 [cm-1]
 ( 0.294694 0.000000 -0.319422 0.000000 -0.557786 0.000000 )
 ( 0.294694 0.000000 -0.319422 0.000000 -0.557786 0.000000 )
     omega( 2) = 0.437450 [THz] = 14.591747 [cm-1]
 ( -0.445392 0.000000 -0.543899 0.000000 0.076157 0.000000 )
 ( -0.445392 0.000000 -0.543899 0.000000 0.076157 0.000000 )
     omega( 3) = 0.437450 [THz] = 14.591747 [cm-1]
 ( 0.463445 0.000000 -0.319599 0.000000 0.427873 0.000000 )
 ( 0.463445 0.000000 -0.319599 0.000000 0.427873 0.000000 )
     omega( 4) = 14.994107 [THz] = 500.149581 [cm-1]
 ( -0.053967 0.000000 -0.110628 0.000000 0.696311 0.000000 )
 ( 0.053967 0.000000 0.110628 0.000000 -0.696311 0.000000 )
     omega( 5) = 14.994107 [THz] = 500.149581 [cm-1]
 ( 0.635522 0.000000 -0.310019 0.000000 0.000000 0.000000 )
 ( -0.635522 0.000000 0.310019 0.000000 0.000000 0.000000 )
     omega( 6) = 14.994107 [THz] = 500.149581 [cm-1]
 ( 0.305286 0.000000 0.625819 0.000000 0.123090 0.000000 )
 ( -0.305286 0.000000 -0.625819 0.000000 -0.123090 0.000000 )
 **************************************************************************
eigenvectors

---
Exercise 1: phonon frequencies at Γ-point for silicon
The acoustic sum rule (ASR):
Due to translational invariance, the zone centre dynamical matrix
should allow a rigid translation of the solid as an eigenvector with
zero eigenfrequency. This leads to the sum rule:
ΣK CKα,K'β = 0
K is atom index
α, β= x, y, z
Numercal inaccuracies lead to violation of accoustic sum rules for
force constant and effective charges.
Reasons:
●Insufficient k-point sampling.
●Large convergence thresholds.
●Small charge density cutoff (ecutrho) for ultrasoft PPs.

---
Exercise 1: phonon frequencies at Γ-point for silicon
Step 3: run dynmat.x with input file dynmat_Si_G.in
We apply ASR rule in this step
(skip step 3 for non-Γ q-point)
&input
     fildyn='si.dynmat_G',
     asr='simple',
     filout='dynmat.out',
     filxsf='dynmat.axsf',
/
Dynamical matrix file
Type of ASR rule
File that stores eigenvalues
and eigenvectors
XSF file: open in Xcrysden
to visualize the modes of vibration
/usr/local/apps/espresso-5.1/bin/dynmat.x < dynmat_Si_G.in > dynmat_Si_G.out

---
Exercise 1: phonon frequencies at Γ-point for silicon
Types of ASR in Quantum ESPRESSO
! asr character indicates the type of Acoustic Sum Rule imposed
! - 'no': no Acoustic Sum Rules imposed (default)
! - 'simple': previous implementation of the asr used
! (3 translational asr imposed by correction of
! the diagonal elements of the dynamical matrix)
! - 'crystal': 3 translational asr imposed by optimized
! correction of the dyn. matrix (projection).
! - 'one-dim': 3 translational asr + 1 rotational asr
! imposed by optimized correction of the dyn. mat. (the
! rotation axis is the direction of periodicity; it
! will work only if this axis considered is one of
! the cartesian axis).
! - 'zero-dim': 3 translational asr + 3 rotational asr
! imposed by optimized correction of the dyn. mat.
! Note that in certain cases, not all the rotational asr
! can be applied (e.g. if there are only 2 atoms in a
! molecule or if all the atoms are aligned, etc.).
! In these cases the supplementary asr are cancelled
! during the orthonormalization procedure (see below).
! Finally, in all cases except 'no' a simple correction
! on the effective charges is performed (same as in the
! previous implementation).

---
Exercise 1: phonon frequencies at Γ-point for silicon
dynmat.out file: Changes in eigenvalues and eigenvectors
diagonalizing the dynamical matrix ...
 q = 0.0000 0.0000 0.0000
 *****************************************************************
     omega( 1) = 0.000000 [THz] = 0.000000 [cm-1]
 ( 0.000000 0.000000 -0.707107 0.000000 0.000000 0.000000 )
 ( 0.000000 0.000000 -0.707107 0.000000 0.000000 0.000000 )
     omega( 2) = 0.000000 [THz] = 0.000000 [cm-1]
 ( -0.707107 0.000000 0.000000 0.000000 0.000000 0.000000 )
 ( -0.707107 0.000000 0.000000 0.000000 0.000000 0.000000 )
     omega( 3) = 0.000000 [THz] = 0.000000 [cm-1]
 ( 0.000000 0.000000 0.000000 0.000000 -0.707107 0.000000 )
 ( 0.000000 0.000000 0.000000 0.000000 -0.707107 0.000000 )
     omega( 4) = 14.987725 [THz] = 499.936680 [cm-1]
 ( 0.000000 0.000000 0.707107 0.000000 0.000000 0.000000 )
 ( 0.000000 0.000000 -0.707107 0.000000 0.000000 0.000000 )
     omega( 5) = 14.987725 [THz] = 499.936680 [cm-1]
 ( 0.000000 0.000000 0.000000 0.000000 -0.707107 0.000000 )
 ( 0.000000 0.000000 0.000000 0.000000 0.707107 0.000000 )
     omega( 6) = 14.987725 [THz] = 499.936680 [cm-1]
 ( -0.707107 0.000000 0.000000 0.000000 0.000000 0.000000 )
 ( 0.707107 0.000000 0.000000 0.000000 0.000000 0.000000 )
 *****************************************************************

---
Exercise 2: phonon dispersion for silicon
- Executables: pw.x and ph.x
- Post processing: q2r.x, matdyn.x, plotband.x
  To run the script: nohup sh run.sh &
Step1: run a scf calculation on the equilibrium structure
Same as step 1 in Exercise 1

---
Exercise 2: phonon dispersion for silicon
Step 2: run ph.x on a grid of q points
Look in si_ph.in file
 &inputph
   outdir='./tmp/',
   prefix='si',
   ldisp=.true.
   nq1=4,nq2=4,nq3=4
   fildyn='si.dynmat',
   tr2_ph=1.0d-14,
   amass(1)=28.086
 /
Specifies that phonon calculations
are on a grid of q-points
4x4x4 grid of q-points
Run: nohup /usr/local/apps/espresso-5.1/bin/ph.x < si_ph.in > si_ph.out &

---
Exercise 2: phonon dispersion for silicon
ph.x generates si.dynmat0 to si.dynmat8 files
si.dynmat0 consists of the q-point grid
si.dynmat1 to si.dynmat8 consist of dynamical matrices for 4x4x4 grid of q-points
Step 3:
This step fourier transforms dynamical matrices from q-space (i.e. si.dynmat0 to si.dynmat8) to real space (R-space) force constant matrix (si444.fc). The q2r.in file
&input
 fildyn='si.dynmat'
 zasr='simple'
 flfrc='si444.fc'
/
/usr/local/apps/espresso-5.1/bin/pw.xq2r.x < q2r.in > q2r.out

---
Exercise 2: phonon dispersion for silicon
Step 4:
This step involves generating the dynamical matrix (eigenvectors and eigenvalues) for an arbitrary q-point from the force constant matrix using Fourier interpolation.
Look in matdyn_Si_disp.in file
 &input
    asr='simple',
    amass(1)=28.0855,
    flfrc='si444.fc',
    flfrq='si.freq',
    q_in_band_form=.true.
 /
5
 0.0000000 0.0000000 0.0000000 10
 0.0000000 0.0000000 1.0000000 10
 0.5000000 0.0000000 1.0000000 10
 0.5000000 0.5000000 0.5000000 10
 0.0000000 0.0000000 0.0000000 1
Force constant matrix file
Output file
For band calculations
List of high symmetry points in 2pi/a followed by number of points between two high symmetry q-points

---
Exercise 2: phonon dispersion for silicon
Step 5: Run plotband.x to generate a file which can be plotted
We will run plotband.x interactively
prompt> /usr/local/apps/espresso-5.1/bin/plotband.x
We plot the band structure using a plotting software

---
Exercise 2: phonon dispersion for silicon
BZ of FCC lattice

---
Exercise 2: phonon dispersion for silicon
Phonon density of states (DOS) using matdyn.x
The matdyn.x executable can also be used to calculate the phonon
density of states
Look in matdyn_Si_dos.in file
&input
    asr='simple',
    amass(1)=28.0855,
    flfrc='si444.fc', flfrq='si.freq.dos'
    dos=.true.,
    fldos='si.dos'
    deltaE=1.d0,
    nk1=4, nk2=4, nk3=4,
 /
Tag for calculating DOS
File with phonon DOS
Energy interval

---
Exercise 3: LO-TO splitting for AlAs
In polar crystals, long range macroscopic electric fields arise that
are associated with long wave longitudinal optical (LO) phonons.
The long range electric fields associated with long-wavelength
LO phonons are responsible for removal of degeneracy between the LO and TO (Transverse Optical) phonons at the Brillouin zone centre (q= 0), and is known as LO-TO splitting.

---
Exercise 3: LO-TO splitting for AlAs
A macroscopic electric field is incompatible with periodic boundary conditions (PBC).
Force constants need to be modified in the case of PBC to account for the
LO-TO splitting.
A non-analytic term involving the effective charges (polarization induced
by lattice distortion) and the dielectric tensor (polarization induced by electric field) is added to the force constants at gamma point.

---
Exercise 3: LO-TO splitting for AlAs
- Executables: pw.x and ph.x
- Post processing: dynmat.x
  To run the script: nohup sh run.sh &
Step1: run a scf calculation on the equilibrium structure
 &system
    ibrav= 2, nat= 2, ntyp= 2,celldm(1)=10.58997,
    ecutwfc =45, ecutrho=180
    occupations='fixed', nbnd=8
 /
 &electrons
    mixing_mode = 'plain'
    mixing_beta = 0.5
    conv_thr = 1.0d-10
 /
Do a calculation with fixed
occupations
Keep small
covergence threshold

---
Exercise 3: LO-TO splitting for AlAs
Step2: run ph.x with alas_ph_G.in input file
&inputph
   outdir='./tmp/',
   prefix='alas',
   fildyn='alas.dynmat_G',
   epsil=.true.,
   tr2_ph=1.0d-14,
   amass(1)= 26.98,
   amass(2)= 74.92,
 /
0.0 0.0 0.0
To calculate born effective
charges and dielectric constant

---
Exercise 3: LO-TO splitting for AlAs
Output in alas_G_ph.out
        Dielectric constant in cartesian axis
        ( 9.224845161 0.000000000 0.000000000 )
        ( 0.000000000 9.224845161 0.000000000 )
        ( 0.000000000 0.000000000 9.224845161 )
        Effective charges (d Force / dE) in cartesian axis
        atom 1 Al
      Ex ( 2.15581 0.00000 0.00000 )
      Ey ( 0.00000 2.15581 0.00000 )
      Ez ( 0.00000 0.00000 2.15581 )
        atom 2 As
      Ex ( -2.17069 0.00000 0.00000 )
      Ey ( 0.00000 -2.17069 0.00000 )
      Ez ( 0.00000 0.00000 -2.17069 )
     Diagonalizing the dynamical matrix
     q = ( 0.000000000 0.000000000 0.000000000 )
 **************************************************************************
     omega( 1) = 0.153627 [THz] = 5.124437 [cm-1]
     omega( 2) = 0.153627 [THz] = 5.124437 [cm-1]
     omega( 3) = 0.153627 [THz] = 5.124437 [cm-1]
     omega( 4) = 10.714684 [THz] = 357.403379 [cm-1]
     omega( 5) = 10.714684 [THz] = 357.403379 [cm-1]
     omega( 6) = 10.714684 [THz] = 357.403379 [cm-1]
 **************************************************************************
ASR not satisfied
No LO-TO splitting

---
Exercise 3: LO-TO splitting for AlAs
Step3: run dynmat.x with dynmat_alas_G.in
&input
     fildyn='alas.dynmat_G',
     asr='simple',
     amass(1)= 26.98,
     amass(2)= 74.92,
     q(1)=1.0, q(2)=0.0, q(3)=0.00,
     filout='dynmat.out',
     filxsf='dynmat.axsf',
/
Direction for approaching
Gamma point (q= 0)
Check output in dynmat_alas_G.out
# mode [cm-1] [THz] IR
    1 0.00 0.0000 0.0000
    2 0.00 0.0000 0.0000
    3 0.00 0.0000 0.0000
    4 357.40 10.7144 5.4432
    5 357.40 10.7144 5.4432
    6 395.39 11.8536 5.4432
LO-TO splitting
2 TO modes and 1 LO mode

---
Exercise 4: phonon dispersion of a metal (Al)
Repeat exercise 2
Notice the ecutwfc, ecutrho, conv_thr, kmesh
Do you think they are converged?
Check how phonons converge with the above parameters.