Hands on session:
POLARIZATION via Berry phase with Quantum ESPRESSO
Sharmila Shirodkar
Jawaharlal Nehru Centre for Advanced Scientific Research
Bangalore

---
Exercises
1. To calculate polarization via Berry phase for symmetric tetragonal BaTiO3
2. To optimize the structure of tetragonal BaTiO3 with displaced Ti atom, and calculate the polarization via Berry phase
3. To determine the Born effective charges from Polarization for Cubic BaTiO3
Asymmetric
Symmetric

---
Steps that are followed
1. Do a total energy calculation that calculates the charge density (scf) with well converged kmesh and ecutwfc
2. Make sure that the system is insulating at every kpoint.
  Berry phase is ill-defined for metals!
3. Run berry phase calculations (nscf) to
  evaluate the Berry phase along k-point strings
4. Total polarization = Ionic part + electronic part
5. Spontaneous polarization= P(asymmetric cell) – P(symmetric cell)

---
Exercise 1: polarization of symmetric tetragonal BaTiO3
Executable: pw.x
To run the script: nohup sh job_sy.sh &
Step1: run a scf calculation on the equilibrium structure
Look at sy.scf.in

---
Exercise 1: polarization of symmetric tetragonal BaTiO3
Step2: run a nscf calculation with sy.bscf.in
/usr/local/apps/espresso-5.1/bin/pw.x < sy.bscf.in > sy.bscf.out
 &control
    calculation = 'nscf'
    restart_mode='from_scratch',
    prefix='symm',
    pseudo_dir = '../../pseudo',
    outdir='tmp-sy'
    lberry=.true.
    gdir = 3
    nppstr = 10
 /
K_POINTS {automatic}
10 10 20 0 0 0
nscf calculation
 For doing Berry phase calculations
direction of the k-point strings in reciprocal space. Allowed values: 1, 2, 3 where 1= first, 2= second, 3=third reciprocal lattice vector
Number of kpoints in the string along gdir
nppstr = nk3

---
Exercise 1: polarization of symmetric tetragonal BaTiO3
In sy.bscf.out
        K-POINTS STRINGS USED IN CALCULATIONS
        ~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~
       G-vector along string (2 pi/a): 0.00000 0.00000 0.97699
       Modulus of the vector (1/bohr): 0.82171
       Number of k-points per string: 10
       Number of different strings : 6
        IONIC POLARIZATION
        ~~~~~~~~~~~~~~~~~~ ============================
    Ion Species Charge Position Phase
  ----------------------------------------------------------------------------
     1 Ba 10.000 0.0000 0.0000 0.0000 0.00000 (mod 2)
     2 Ti 12.000 0.5000 0.5000 0.5118 0.00000 (mod 2)
     3 O 6.000 0.5000 0.5000 0.0000 0.00000 (mod 2)
     4 O 6.000 0.5000 0.0000 0.5118 -1.00000 (mod 2)
     5 O 6.000 0.0000 0.5000 0.5118 -1.00000 (mod 2)
  ----------------------------------------------------------------------------
        IONIC PHASE: 0.00000 (mod 2)
nppstr
Depends on nk1 and nk2
No contribution
from ions!

---
Exercise 1: polarization of symmetric tetragonal BaTiO3
In sy.bscf.out
        ELECTRONIC POLARIZATION	~~~~~~~~~~~~~~~~~~~~~~~
        Note: (mod 1) means that the phases (angles ranging from
        -pi to pi) have been mapped to the interval [-1/2,+1/2) by
        dividing by 2*pi; (mod 2) refers to the interval [-1,+1)
=============================================
 Spin String Weight First k-point in string Phase
----------------------------------------------------------------------------
  up 1 0.040000 0.0000 0.0000 0.0000 0.00000 (mod 1)
  up 2 0.160000 0.0000 0.2000 0.0000 0.00000 (mod 1)
 ...
  Up 5 0.320000 0.2000 0.4000 0.0000 0.00000 (mod 1)
  Up 6 0.160000 0.4000 0.4000 0.0000 0.00000 (mod 1)
----------------------------------------------------------------------------
 down 1 0.040000 0.0000 0.0000 0.0000 0.00000 (mod 1)
 down 2 0.160000 0.0000 0.2000 0.0000 0.00000 (mod 1)
...
 Down 5 0.320000 0.2000 0.4000 0.0000 0.00000 (mod 1)
 Down 6 0.160000 0.4000 0.4000 0.0000 0.00000 (mod 1)
----------------------------------------------------------------------------
nk1
and nk2
The total phase and polarization in symmetric structure = 0
No contribution from electrons!

---
Exercise 2: polarization of asymmetric tetragonal BaTiO3
Executable: pw.x
Step1: Displace Ti atom in +z direction and relax the structure. Look in relax.in file
&control
    calculation = 'relax'
    restart_mode='from_scratch',
    prefix='asymm-relax',
    tstress = .true.
    tprnfor = .true.
    pseudo_dir = '../../pseudo',
    outdir='tmp'
 /
ATOMIC_POSITIONS {crystal}
 Ba 0.0000 0.0000 0.0000
  Ti 0.5000 0.5000 0.5200
   O 0.5000 0.5000 0.0000
   O 0.5000 0.0000 0.5000
   O 0.0000 0.5000 0.5000
Structural relaxation calculation
Ti atom is displaced along z
/usr/local/apps/espresso-5.1/bin/pw.x < relax.in > relax.out

---
Exercise 2: polarization of asymmetric tetragonal BaTiO3
Look at the final relaxed co-ordinates in relax.out file
ATOMIC_POSITIONS (crystal)
Ba 0.000000000 0.000000000 0.020604613
Ti 0.500000000 0.500000000 0.530311403
O 0.500000000 0.500000000 -0.015428482
O 0.500000000 0.000000000 0.492256232
O 0.000000000 0.500000000 0.492256232
Use the above co-ordinates in asy.scf.in and asy.bscfx.in,
asy.bscfy.in and asy.bscfz.in files

---
Exercise 2: polarization of asymmetric tetragonal BaTiO3
Step2: Repeat Steps 2 and 3 from exercise 1
In asy.bscf.out
        IONIC POLARIZATION
        ~~~~~~~~~~~~~~~~~~ ============================
    Ion Species Charge Position Phase
  ----------------------------------------------------------------------------
     1 Ba 10.000 0.0000 0.0000 0.0211 0.20605 (mod 2)
     2 Ti 12.000 0.5000 0.5000 0.5428 0.36374 (mod 2)
     3 O 6.000 0.5000 0.5000 -0.0158 -0.09257 (mod 2)
     4 O 6.000 0.5000 0.0000 0.5038 0.95354 (mod 2)
     5 O 6.000 0.0000 0.5000 0.5038 0.95354 (mod 2)
  ----------------------------------------------------------------------------
        IONIC PHASE: 0.38429 (mod 2)
Finite contribution
from ions!

---
Exercise 2: polarization of asymmetric tetragonal BaTiO3
In asy.bscfz.out
        ELECTRONIC POLARIZATION	~~~~~~~~~~~~~~~~~~~~~~~
        Note: (mod 1) means that the phases (angles ranging from
        -pi to pi) have been mapped to the interval [-1/2,+1/2) by
        dividing by 2*pi; (mod 2) refers to the interval [-1,+1)
=============================================
 Spin String Weight First k-point in string Phase
----------------------------------------------------------------------------
  up 1 0.040000 0.0000 0.0000 0.0000 0.06891 (mod 1)
  up 2 0.160000 0.0000 0.2000 0.0000 0.03158 (mod 1)
 ...
  up 5 0.320000 0.2000 0.4000 0.0000 -0.02818 (mod 1)
  up 6 0.160000 0.4000 0.4000 0.0000 -0.05090 (mod 1)
----------------------------------------------------------------------------
 down 1 0.040000 0.0000 0.0000 0.0000 0.06891 (mod 1)
 down 2 0.160000 0.0000 0.2000 0.0000 0.03158 (mod 1)
...
 down 5 0.320000 0.2000 0.4000 0.0000 -0.02818 (mod 1)
 down 6 0.160000 0.4000 0.4000 0.0000 -0.05090 (mod 1)
----------------------------------------------------------------------------
ELECTRONIC PHASE: -0.01845 (mod 2)
Finite contribution from electrons!
Total polarization is non-zero along z!

---
Exercise 2: polarization of asymmetric tetragonal BaTiO3
In asy.bscf.out
        SUMMARY OF PHASES
 ~~~~~~~~~~~~~~~~~
        Ionic Phase: 0.38429 (mod 2)
        Electronic Phase: -0.01845 (mod 2)
        TOTAL PHASE: 0.36584 (mod 2)
        VALUES OF POLARIZATION
        ~~~~~~~~~~~~~~~~~~~~~
        The calculation of phases done along the direction of vector 3
        of the reciprocal lattice gives the following contribution to
        the polarization vector (in different units, and being Omega
        the volume of the unit cell):
        P = 2.7973956 (mod 15.2930243) (e/Omega).bohr
        P = 0.0065551 (mod 0.0358362) e/bohr^2
        P = 0.3747686 (mod 2.0488144) C/m^2
        The polarization direction is: ( 0.00000 , 0.00000 , 1.00000 )
Sum of electronic
and ionic phases
Sum of electronic
and ionic phases
P= -ie/(2π3)*berry phase
Polarization
quantum
Polarization in
different units

---
Exercise 2: polarization of asymmetric tetragonal BaTiO3
Polarization of tetragonal BaTiO3
P(asymmetric phase)- P(symmetric phase)
= 37 μC/cm2 - 0 μC/cm2
= 37 μC/cm2
Why is the polarization not same as in experiments (26 μC/cm2 )?
Check the convergence of P with nppstr and nk1, nk2

---
Exercise 3: Born Effective charges for cubic BaTiO3
Step1: Look at scf.in
The Ti atom is displaced by +z direction by 0.01a
Step2: Look at bscf.in
Now run a berry phase calculation along gdir=3
Step3: Calculate the Born Effective charge
        dP
       Z* = Omega ----
        dr